## Slide 1: Three scales of ice
M
Molecular
Atmospheric

## Slide 2: Here I’ll be focusing on the molecular and mesoscopic
M
Molecular
Atmospheric
Part I:
How do growing ice surfaces remain flat?
Part II:
How do they become rough? (Actually, what is roughness?)

## Slide 3
We’d like to describe these behaviors in a way pioneered by BCF (and others) …

## Slide 4
We’d like to describe these behaviors in a way pioneered by BCF (and others) …
… But we can’t because of the pesky quasi-liquid layer

## Slide 5
Which led to a paper back in 2016 in which we tried to span those two scales
We have a mathematical criterion
prismatic surface
Molecular order parameters let us quantify , , and therefore
prismatic surface
basal surface

## Slide 6
Here are the kind of numerical experiments we did
We have a mathematical criterion
The time for this simulation is picoseconds, but after a few nanoseconds, we could get “equilibrium” thicknesses of the QLL.
basal surface

## Slide 7
We found a periodic variation in as a function of
“
(thinner)
“-surface II”
(thicker)

## Slide 8
We think we understood why the variation occurs
surface I is thin because it has just the right number of interstitial molecules.

## Slide 9
A rough description of that variation as a function of

## Slide 10
The simulations also predicted that surface II is more volatile than surface I.
surface II
surface I
More volatile => higher => higher chemical potential, which will affect the rate at which the two surfaces will be able to hold onto new water molecules that just landed from the vapor phase.

## Slide 11
Scaling up to the mesoscale (or SEM scale) led to a pair of partial differential equations …
… of which I’ll be describing a revised version here.

## Slide 12
Two coupled PDEs and the processes they’re meant to represent

## Slide 13
Interconversion of quasi-liquid with the underlying ice lattice

## Slide 14
Interconversion of quasi-liquid with the underlying ice lattice
is the equilibrium thickness of the QLL. Recall that MD said
So .

## Slide 15
Surface diffusion of the QLL

## Slide 16
Surface diffusion of the QLL
is estimated from MD.
is the angle the ice surface makes with respect to the prismatic frame.

## Slide 17
Exchange with the overlying water vapor

## Slide 18
Exchange with the overlying water vapor
is the rate at which water vapor hits the surface.
is the local supersaturation.

## Slide 19
A little more explanation of … it depends on the overlying vapor pressure,
Ice crystal
(2D)
Higher
Supersaturation is greater at facet corners

## Slide 20
But also depends on the state of the QLL
Define a variable so that:
to represent surface II (thick, more volatile)
to represent surface I (thin, less volatile)
(accomplished by ). Then the actual supersaturation felt at any position on the surface is
where is the difference in equilibrium supersaturation between surface I and surface II.

## Slide 21
OK, let’s look at some results – solving the PDE starting with a flat surface

## Slide 22
OK, let’s look at some results – solving the PDE starting with a flat surface

## Slide 23
Considering and together => steps correspond to mainly surface I (thin QLL)

## Slide 24
Considering and together => terraces correspond to mainly surface II (thick QLL)

## Slide 25
After long enough time, a stable limit cycle emerges
stable limit cycle achieved after

## Slide 26
Mechanism: surface diffusion modifies the surface in response to vapor inhomogeneity
Diffusion of quasiliquid from terraces into steps makes steps a little more more volatile.
Increased volatility is more pronounced at facet corners because steps are closer together there.
Greater volatility at corners compensates for higher imposed there.

## Slide 27
The same mechanism works with any smooth inhomogeneity in the overlying vapor field
Imposed supersaturation
Higher at facet corners
Higher at facet center
Limit cycle with convex curvature
Limit cycle with concave curvature
Shape of the converged surface

## Slide 28
1. Smooth faceted growth is the result of stable limit cycles that form as an emergent property of the dynamics of ice growth.
2. This emergence accommodates any smooth inhomogeneity in the overlying vapor field.
3. Modest curvature + equal growth rates across a facet => what appears (at the mesoscale) as faceted growth.
Take-home lesson from Part 1: limit cycling explains faceted growth

## Slide 29: On to Part II
Molecular scale
(from scanning electron microscopy)
Part I:
How do growing ice surfaces remain flat?
Part II:
How do they become rough? (Actually, what is roughness?)

## Slide 30
Hypothesis: maybe roughness is “just” microfacets of other angles

## Slide 31
Why? Optical microscopy tells us there are characteristic peak-to-peak distances
Regarding those stripes (roughness):
The peak-to-peak distance here is m
The vertical relief is (sadly) indeterminate

## Slide 32
SEM/GNBF gives us the vertical relief
Vacuum

## Slide 33
SEM/GNBF gives us the angles too
Horizontal Peak-to-peak distance m
Vertical relief m
=> Slope

## Slide 34
SEM/GNBF gives us the angles too
Horizontal Peak-to-peak distance m
Vertical relief m
=> Slope

## Slide 35
To enable microfaceting in the PDE, the basic idea is that the slope of the surface is key …
Ice surface
Prismatic monolayer (
At this point, the surface slope is close to the prismatic plane, so that point is “prismatic-like”.

## Slide 36
Red lines indicate successive layers of a “pyramidal” facet plane
At this point, the surface slope is close to a positively-sloped (“pyramidal”) plane, so that point is “pyramidal-like”.

## Slide 37
There’s also a negatively-sloped “pyramidal” facet plane
At this point, the surface slope is close to a negatively-sloped facet plane (“pyramidal”), so that point is “-pyramidal-like”.

## Slide 38
Keep the form of the PDE, but replace and with slope-sensitive values

## Slide 39
For : First we need to compute the layer thicknesses () at each grid point
E.g, at the dot, and
Generally:

## Slide 40
We’ll skip the next few slides
There’s a lotta math in the next few slides, we’ll come back to them later.

## Slide 41
For : Then we’ll weight them (“”)

## Slide 42
For : Each facet angle gets an and

## Slide 43
For : Then we’ll weight them (“”)

## Slide 44
We need those weights &
Slopes:
Each grid point has a slope ()

## Slide 45
Assign the weights according to the slope of the surface
Here, , so the grid point aligns with the positively-sloped (“pyramidal”) facet
Slopes:

## Slide 46
Assign the weights according to the slope of the surface
Here, , so we’d say the grid point aligns best with the original facet (prismatic)
Slopes:

## Slide 47
Assign the weights according to the slope of the surface
so the grid point aligns with the negatively-sloped facet
Slopes:

## Slide 48
Assign weights using sigmoid functions (, , )

## Slide 49
Pick up again below here

## Slide 50
Each grid point is assigned a set of weights (, , )

## Slide 51
Replace and with and

## Slide 52
Results: given the same parameters, the microfacet-enabled PDE results in limit cycles a lot like the prismatic-only version
Original PDE
(at )
microfacet-enabled
(at )
Number of steps

## Slide 53
Non-growable microfaceting, high-deposition rate
Notes: of these microfacets is high enough that:
Supersaturation is less than that of the equilibrium value of ’s surface II => the microfacets can’t grow
Supersaturation is greater than the equilibrium value of ’s surface I => the microfacets can’t ablate either
=> A steady state results.

## Slide 54
Non-growable microfaceting, high-deposition rate
Notes: of these microfacets is high enough that:
Supersaturation is less than that of the equilibrium value of ’s surface II => the microfacets can’t grow
Supersaturation is greater than the equilibrium value of ’s surface I => the microfacets can’t ablate either
=> A steady state results.

## Slide 55
Growable microfaceting, fast-growth conditions
Notes: of these microfacets is low enough that even ’s surface II can grow => A limit cycle results.

## Slide 56
Growable microfaceting, fast-growth conditions
Notes: of these microfacets is low enough that even ’s surface II can grow => A limit cycle results.

## Slide 57
Non-growable microfaceting, high-deposition rate
Notes: of these microfacets is high enough that:
Supersaturation is less than that of the equilibrium value of ’s surface II => the microfacets can’t grow
Supersaturation is greater than the equilibrium value of ’s surface I => the microfacets can’t ablate either
=> A steady state results.

## Slide 58
Non-growable microfaceting, high-deposition rate
Notes: of these microfacets is high enough that:
Supersaturation is less than that of the equilibrium value of ’s surface II => the microfacets can’t grow
Supersaturation is greater than the equilibrium value of ’s surface I => the microfacets can’t ablate either
=> A steady state results.

## Slide 59
Growable microfaceting, high-deposition rate
Notes: of these microfacets is low enough that even ’s surface II can grow => A limit cycle results.

## Slide 60
Take-home lessons
From Part I:
1. Smooth faceted growth is the result of stable limit cycles that form as an emergent property of the dynamics of ice growth.
2. This emergence accommodates any smooth inhomogeneity in the overlying vapor field.
3. Modest curvature + equal growth rates across a facet => what appears (at the mesoscale) as faceted growth.
From Part II:
1. Roughness is consistent with microfacet formation modulating otherwise flat faceted surfaces.
2. Microfacets stabilize the surface in that they enable steady-state profiles in some conditions, and limit cycle profiles in others.
3. Available in situ (visible, SEM/GNBF) experiments suggest a predominance of microfaceting on prismatic facets in the principle (c) axis direction.

## Slide 61
Going forward …
Model:
How do the surrounding vapor fields really vary for growing or ablating crystals?
What insights might a Fourier formulation provide?
What about a PDE for two-dimensional crystal surfaces?
Observations:
What range are observed microfacet angles?
What happens in subsaturated conditions?
More broadly:
Can we use this theory to predict optical properties of cirrus ice in a way that’s useful to climate science?
Atmospheric

## Slide 62
Thanks for listening!

## Slide 63
We do get positive curvature on “flat” basal facets, although it’s a lot bigger and bumpier than stable limit-cycle theory predicts

## Slide 64
The beginnings of hollowing when gets big (higher temperature)

## Slide 65
Molecular Dynamics studies of ice surfaces
December 2016

## Slide 66
microfaceting enabled, after 10 seconds simulated time (w/o D correction)
The vertical scale is in here, x1000s greater than what I showed you before; it would be visible on a microscopic (e.g., SEM) scale.
It would develop a steady state.

## Slide 67
Steps are characterized by thin quasiliquid (i.e., surface I)
surface I

## Slide 68
Steps are characterized by thin quasiliquid (i.e., surface I)
surface I

## Slide 69
Steps are characterized by thin quasiliquid (i.e., surface I)
surface I

## Slide 70
Terraces are characterized by thick quasiliquid (i.e., surface II)
surface II

## Slide 71
Terraces are characterized by thick quasiliquid (i.e., surface II)
surface II

## Slide 72
Terraces are characterized by thick quasiliquid (i.e., surface II)
surface II